Inflatable Boat Material Reference Chart

Manufacturer					Material

Achilles						Hypalon

AIRE							PVC

Avon							Hypalon

Campway						Hypalon

Hyside							Hypalon

Incept							PVC

Maravia						PVC

Marnenturn						Hypalon

NRS							Hypalon

NRS Bandit Series					Urethane

Odyssey						PVC

Pro Advantage						Hypalon

Riken							Hypalon

Rogue River						Hypalon

Sevylor						PVC

Sotar							Urethane

Star							PVC

Tributary						PVC

Tributary lks						PVC

Udisco							Neoprene (hypalon adhesive)

Wing							PVC

Zodiac (pre 1985)					Hypalon

Zodiac (post 1985)					PVC